SABANCI UNIVERSITY

GLASS SCIENCE AND TECHNOLOGY COURSE

MAT 422 - 522

A senior level course devoted to the understanding of commercial (SLS) silicate glass as a material and its technology of production. A modular course taught in theory and practice in collaboration with the glass industry experts in Turkey.

Recommended reading:

- The Handbook of Glass Manufacture,  F.Tooley, Tooley, New York : Books for Industry, [1974]

- Fundamentals of Inorganic Glasses, A. K. Varshneya, Academic Press Inc. 1994, CA, USA

- Glasses and Their Applications, H.Rawson, The Institute of Metals, 1991

- Glass Furnaces Design, Construction and Operation, Wolfgang Trier, Socitety of Glass Technology, Sheffield, UK, 2000 (translated by K.L. Loewenstein from Glassschmelzöfen: Konstruktion und Betreibsverhalten, W. Trier, Springer Verlag, 1984).

- Handbook of Glass ed. by J. David Musgraves, Juejun Hu, Laurent Calvez, Springer 2019

Chapter 1:  Glass and Glassy State					Week #8 (Feb. 26, 2021)

- Introduction

- History

- Definition of glass

- Glass formation

- Theories related to glass formation

Duration:  1 week / 3 lectures;					Instructor: Melek Orhon

Chapter 2: Glass Compositions and Properties                             Week #9, 10, 11 & 12 (March 05, 12, 19, 26 2021)

- Glass compositions (March 05) by Melek Orhon

- Viscosity

  - Importance of viscosity in glass production

  - Factors affecting viscosity

- Density

- Thermal expansion

- Effect of composition on thermal expansion

- Temporary and permanent stresses

- Annealing

- Mechanical properties (March 12) by Melek Orhon

- Basic principles: Stress- strain, elasticity, etc.

- Mechanical strength of glass

- Griffith model

- Subcritical crack growth, dynamic/static fatigue

- Measuring strength

- Hardness

- Tempering

- Surface Tension (March 19) by Atilla Ünsal

- Thermal and Electrical Properties

  - Heat capacity

  - Thermal conductivity and Heat transfer

  - Electrical conductivity

- Chemical durability  (March 19) by Melek Orhon

- Corrosion reactions/weathering

- Effect of chemical composition and temperature

- Dishwasher resistance

- Optical properties (March 26) by Melek Orhon

  - Glass and electromagnetic radiation

  - Absorption-transmission-reflection-dispersion-scattering in glass

  - Color generation

  - Decolorizing

  - Defining color (color coordinates)

Duration: 4 weeks/ 12 lectures;				Instructor: Melek Orhon, Atilla Ünsal

Mid-term Exam #1                                                                                            Week #13

Chapter 3: Raw Materials and Batch				Week #13 &17 (April 02, 26 2021)

- Raw materials (April 02) by Melek Orhon

- Common raw materials

- Raw material specifications

- Batch Calculations

- Batch preparation (April 26) by Atilla Ünsal

  - Properties of granular materials

  - Bulk solids

  - Preparation of raw materials

  - Handling and transport

  - Segregation

  - Batch plants

  - Dosing

  - Mixing

  - Batch charging

Duration: 2 weeks / 6 lectures;			Instructors: Melek Orhon, Atilla Ünsal

Chapter 4:  Glass Melting 						Week #15 &16 (April 09, 16)

- Glass Redox (April 09, 16)

- Definition

- Glass redox and color

- Calculating/ measuring redox

- Melting

  - Batch melting

  - Melting energy

  - Parameters affecting reaction rates (Melting temperature, particle size of raw materials, glass composition)

- Fining

  - Gases in glass (physical and chemical dissolution)

  - Formation of bubbles

  - Bubble removal (primary and secondary fining)

  - Bubbles as a defect in glass

- Homogenizing

- Conditioning

Duration: 2 weeks / 6 lectures; 					Instructor: Melek Orhon

Chapter 5: Furnace Technology				Week #18, 20 & 21 (May 07, 21 & 28  2021)

- Furnace Types - Discontinuous/Continuous

- Furnace Structure – Refractories, steelwork

- Heat transfer/Heat exchangers (Regenerator/Recuperators)

- Combustion and firing

- Electric heating and furnaces

- Energy management

- Environmental issues and abatement

- Emerging melting technologies

- Glass Forming – Floating, fiberizing, moulding (PB/PP/NNPB)

- Course Review & QA

Duration: 3 weeks/ 9 lectures;				Instructor: Atilla Ünsal

Term Project                                                                                              Submission    May 31 2021

Mid-term Exam #2                                                                                 Week #22

Spring Semester Academic Calendar:

- Courses ending - May 28

- Final entry date of the term results - June 16

Quizes  %25

Midterm % 25 each

Term Project %25