SABANCI UNIVERSITY

GLASS SCIENCE AND TECHNOLOGY COURSE

MAT 422 - 522

A senior level course devoted to the understanding of commercial (SLS) silicate glass as a material and its technology of production. A modular course taught in theory and practice in collaboration with the glass industry experts in Turkey.

Recommended reading:

- The Handbook of Glass Manufacture,  F.Tooley, Tooley, New York : Books for Industry, [1974]

- Fundamentals of Inorganic Glasses, A. K. Varshneya, Academic Press Inc. 1994, CA, USA

- Glasses and Their Applications, H.Rawson, The Institute of Metals, 1991

- Glass Furnaces Design, Construction and Operation, Wolfgang Trier, Socitety of Glass Technology, Sheffield, UK, 2000 (translated by K.L. Loewenstein from Glassschmelzöfen: Konstruktion und Betreibsverhalten, W. Trier, Springer Verlag, 1984).

- Handbook of Glass ed. by J. David Musgraves, Juejun Hu, Laurent Calvez, Springer 2019

Chapter 1:  Glass and Glassy State					Week #10 (March 4, 2022)

- Introduction

- History

- Definition of glass

- Glass formation

- Theories related to glass formation

Duration:  1 week / 3 lectures;					Instructor: Melek Orhon

Chapter 2: Glass Compositions and Properties                           Week #11, 12, 13 & 14 (March 11, 18, 25 & April 1 2022)

- Glass compositions (March 11) by Melek Orhon

- Viscosity

  - Importance of viscosity in glass production

  - Factors affecting viscosity

- Density

- Thermal expansion

- Effect of composition on thermal expansion

- Temporary and permanent stresses

- Annealing

- Mechanical properties (March 18) by Melek Orhon

- Basic principles: Stress- strain, elasticity, etc.

- Mechanical strength of glass

- Griffith model

- Subcritical crack growth, dynamic/static fatigue

- Measuring strength

- Hardness

- Tempering

- Optical properties (March 25) by Melek Orhon

  - Glass and electromagnetic radiation

  - Absorption-transmission-reflection-dispersion-scattering in glass

  - Color generation

  - Decolorizing

  - Defining color (color coordinates

- Surface Tension (April 1) by Atilla Ünsal

- Thermal and Electrical Properties

  - Heat capacity

  - Thermal conductivity and Heat transfer

  - Electrical conductivity

- Glass Surface & Chemical Durability (April 1) by Melek Orhon

  - Definition of surface

  - Structure of glass surface and bulk glass

  - Formation of glass surface

- Corrosion reactions/weathering

- Effect of chemical composition and temperature

- Dishwasher resistance

Duration: 4 weeks/ 12 lectures;		                       Instructors: Melek Orhon, Atilla Ünsal

Mid-term Exam #1                                                                                 Week #15 (April 8, 2022)

Chapter 3: Raw Materials and Batch				Week #15 &16 (April 8, 15 2022)

- Raw materials (April 8) by Melek Orhon

- Common raw materials

- Raw material specifications

- Batch Calculations

- Batch preparation (April 15) by Atilla Ünsal

  - Properties of granular materials

  - Bulk solids

  - Preparation of raw materials

  - Handling and transport

  - Segregation

  - Batch plants

  - Dosing

  - Mixing

  - Batch charging

Duration: 2 weeks / 5 lectures;			Instructors: Melek Orhon & Atilla Ünsal

Chapter 4:  Glass Melting 						Week #17 &18 (April 22, 29 2022)

- Glass Redox

- Definition

- Glass redox and color

- Calculating/ measuring redox

- Melting

  - Batch melting

  - Melting energy

  - Parameters affecting reaction rates (Melting temperature, particle size of raw materials, glass composition)

- Fining

  - Gases in glass (physical and chemical dissolution)

  - Formation of bubbles

  - Bubble removal (primary and secondary fining)

  - Bubbles as a defect in glass

- Homogenizing

- Conditioning

Duration: 2 weeks / 6 lectures; 					Instructor: Melek Orhon

Chapter 5: Furnace Technology				Week # 20, 22 (May 13, 27 2022)

- Furnace Types - Discontinuous/Continuous

- Furnace Structure – Refractories, steelwork

- Heat transfer/Heat exchangers (Regenerator/Recuperators)

- Combustion and firing

- Electric heating and furnaces

- Energy management

- Environmental issues and abatement

- Emerging melting technologies

- Glass Forming – Floating, fiberizing, moulding (PB/PP/NNPB)

- Course Review & QA

Duration: 2 weeks/ 6 lectures;				                               Instructor: Atilla Ünsal

Şişecam Plant Trip                                                                                                  Week # 21 (May 20 2022)

Duration: 1 day

Career Opportunities for Material Science Graduates at Şişecam              Week # 21 (May 20 2022)

Duration:  1 lecture;                                                                      Presentation by:  Ebru Kahraman & Nihal Eren

Chapter 6: Thin Film Coatings on Glass & Glass Surface Characterization       Week # 23, 24 (June 3, 10 2022)

- Basics of optical thin films and optical design (June 3, 10) by Dr. Burak Okan

- Interference in Thin Films

- Optical Design of Multilayer Thin Films with the Transfer Matrix Approach

- Primary Applications of Coatings on Glass

- Passive Solar Reflective Coatings

- Low Emissivity Coatings

- Antireflection Coatings

- Self-cleaning and Antimicrobial Coatings

- Performance Measurements and Characterization

- Optical Performance (UV/Visible/Solar Transmission, Reflection and Absorption)

- Basics of Color Science

- Emissivity and Sheet Resistance

- Heat Transfer in Insulated Glass Units: Overall Heat Transfer and Solar Heat Gain Characteristics

- Deposition Technologies for Large Area Applications

- Atmospheric Pressure Coating Technologies (Chemical Vapor Deposition, Sol-Gel technology)

- Vacuum Coating Technologies (Magnetron Sputtering)

- Characterization of glass surface (June 10) by Dr. Tuncay Turutoğlu

  - Surface characterization techniques

  - Applications on glass surface

Duration:  2 weeks / 6 lectures;                                                     Instructors:  Dr. Burak Okan & Dr. Tuncay Turutoğlu

Mid-term Exam #2                                                                                 Week # 25                                     Date TBA

Term Project                                                                                           Submission & Presentation       Date TBA

Spring Semester 2022 Academic Calendar:

- Courses Commence – March 4

- Courses ending - June 10

- Final entry date of the term results - June 29

Quizzes %25, Midterms % 25 each, Term Project %25