MAT 408 Introduction to Ceramics

2022 Fall

Lectures, Discussions and (processing) Labs related to Ceramic materials

Instructor:	Dr. Mehmet Ali Gulgun

(office hours: xxx ) FENS 2055

TA:			Kosar Hassan Nezhad, kosar@sabanciuniv.edu

Course Text:		Lecture notes

excerpts from	Physical Ceramics by Chiang et al.

Introduction to Ceramics by Kingery et al.

Ceramic Materials by CB Carter and MG Norton

Introduction to Glass Sci. and Technology by Shelby

Recommended textbooks are:

Physical Ceramics (1997), by Y-M. Chiang, D. Birnie III, and W. D. Kingery, Wiley MIT Series

Introduction to Ceramics (1976), by W. D. Kingery, H. K. Bowen, and D.R. Uhlmann, Wiley Interscience

Ceramic Materials:Science and Engineering (2007), by C.B. Carter and M. G. Norton, Springer

J. S. Reed, Principles of Ceramics Processing, Wiley Interscience, 1995.

Meeting times:	Tuesdayss MAT 408 Class 013:40 pm-14:30 pm FENS L027

Wednesdays  MAT 408 Class 10:40 am-12:30 pm FENS L035

Extra hours for Phase equilibria (maybe)

Meeting place:		Labs will be to be arranged

Important Dates:

Midterm I 		end of October

Midterm II		end of November

Midterm III		end of December

Grading:		80 % Midterms

20 % Homeworks and quizzes

Contents:		Structure of ceramics (weeks 1-2)

History of ceramics and Cement

Atoms, bonds, stability and coordination

Crystalline structures (Review of ENS205 knowledge)

Oxide structures

Covalent ceramics

Silicates

Clays

Polymorphism

Structure of glass (weeks 2-3)

Network formers vs. network modifiers

Properties of glasses

Commercial glass compositions

Key players in commercial glass and their job

Miscibility gap

Raw materials

Defects in Ceramics (weeks 5-6)

Point, line and planar defects

Intrinsic versus extrinsic defects

Describing defects : Kroger – Vink Notation

Association of defects and defect pairs

Interaction of defects

Electronic structure

Transport Phenomena (weeks 7-8)

Atomic Mobility

Diffusion: A thermally activated process

Types of diffusion

Electrical Transport										Ionic versus electronic conductivity

Phase equilibria (optional)

Development of microstructures in ceramics (9-11)

Surface tension and energy

Curved surfaces, grain boundaries

Solute segregation and phase separation

Wetting and dihedral angles

Nucleation

Sintering and vitrification

Liquid phase sintering

Stages of sintering

Grain growth and coarsening

Grain boundary migration

Contents:		Properties of Ceramics  (12-14)

Thermal properties and stresses

Plastic deformation and creep

Strength and toughness

Brittle fracture

Fracture toughness and stresses concentration

Toughening ceramics

Dielectric properties

Dielectric constant and loss factor

Dielectric strength

Ferroelectric ceramics

Magnetic properties

Ferrites : hard and soft

Optical properties

Refractive index and dispersion

Reflectance

Opacity and translucency

Absorption and color