# Sabanci University

# Faculty of Engineering and Natural Sciences

# MAT 48004/68004. Polymer Matrix Composites

## Course Syllabus

Semester		: Fall 2022-2023

Instructor		: Assoc. Prof. Dr. Bekir Dızman

Assistants		: Asu Ece Ateşpare, Negar Amirhaghian, Saeed Salamat Gharamaleki

Exams and Grading	: 2 Midterms/Take-home exams/Presentations (30% each)

Final Exam/Take-home exam/Presentation (40%)

Textbook                    : An Introduction to Poymer Matrix Composites (Mustafa Akay)

| Weeks | Subject | Exams/Presentations |
| --- | --- | --- |
| 1 | Introduction, history and classification of composites |  |
| 2 | PMC constituents: fibers |  |
| 3 | PMC constituents: matrices (thermoplastics) |  |
| 4 | PMC constituents: matrices (thermosets) |  |
| 5 | Fiber-matrix interface, fiber arrangement, fiber and matrix content, void content | Midterm 1/Presentation 1 |
| 6 | Processing and forming methods: open-mold processes (hand lay-up, spray lay-up, prepreg, vacuum bag and autoclave, filament winding, bladder molding/pressure bag molding) |  |
| 7 | Processing and forming methods: wood-plastic composites, other processing considerations (machining, joining, repair) |  |
| 8 | Estimation of mechanical properties: continuous-fiber and short-fiber composites |  |
| 9 | Estimation of mechanical properties: failure mechanisms (debonding, fiber pullout) | Midterm 2/Presentation 2 |
| 10 | Mechanical and thermal properties: tensile, compressive, flexural, shear, impact and fracture toughness properties, bearing strength, fatique and wear | - |
| 11 | Mechanical and thermal properties: bearing strength, fatigue and wear |  |
| 12 | Mechanical and thermal properties: DSC, DMA, TGA, environmental effects on properties, non-destructive evaluation |  |
| 13 | Applications (aerospace, wind turbine blades, building and construction, sports and leisure, bioengineering, transportation, sensors) |  |
| 14 | Materials selection (lightweighing, recycling, health & safety) | Final exam/Presentation 3 |

## Rules

- Attendance to all classes is required and will change the grading as follows:

  - Full attendance (≤ 3 misses) will be awarded with one grade higher (i.e.,  A- ( A)

  - Partial attendance (= 4-7 misses ) will not affect grading (i.e.,  A- (  A-)

  - Poor attendance (> 7 misses) will result in one grade lower (i.e.,  A-  (  B+)

- Exams will be returned one week after they are given. Late returns will get a 20% reduction in the grade.

- Cellphones are not allowed during the class hours.