SABANCI UNIVERSITY

FACULTY OF ENGINEERING AND NATURAL SCIENCES

MATERIALS SCIENCE AND ENGINEERING PROGRAMME

MAT 308 PHASE EQUILIBRIA (3+0)

COURSE DESCRIPTION

Thermodynamic and Phase Equilibria; One Component System Phase Diagrams; Two Component System Phase Diagrams: Binary eutectic, Intermediate compounds, Solid solution, Liquid immiscibility; Determination of Phase Diagrams: Experimental methods, Thermodynamic estimations and calculations; Ternary Systems: Method of determining composition, Isoplethal studies in ternary systems, Binary and ternary intermediate compounds, Solid solutions;

COURSE AIM

The aim of the course is to provide a sound foundation in the basic facts and concepts of phase equilibria for materials engineers.

LEARNING OUTCOMES AND SUB-ACCOMPLISHMENT

- The importance of phase diagrams in materials science and engineering will be able to be defined.

- The main definitions and terms of phase diagram will be able to be explained.

a) The terms of system, phase, equilibrium, components, degrees of freedom, phase rule are defined.

b) These terms are applied in materials science and engineering field.

3. 	In which conditions materials are stable will be interpreted in the unary systems by using pressure and temperature diagram.

- Pressure and temperature diagrams are defined in unary systems.

b) The terms of phase diagrams are applied in the unary systems which are used in materials science and engineering field.

c) These unary systems are compared and interpreted each others

4. 	Binary systems will be able to be composed by using unary systems.

a) Binary systems are designed by using unary systems.

b) These systems are drawn and interpreted

5. 	Problems will be able solved in binary systems by using composition and temperature diagram.

a) Composition and temperature diagrams are defined in binary systems.

b) The formations of congruently-incongruently melted intermediate compounds and

solid solutions are defined in binary systems.

- Different reaction types are defined in binary systems.

- Calculations on cooling and heating are done in binary systems.

- Composition and temperature diagrams are composed by using (G-T graphics.

- The terms of phase diagrams are applied in the binary systems which are used in

materials science and engineering field.

h) These binary systems are compared and interpreted.

6. 	Ternary systems will be able to be composed by using binary systems.

a) Ternary systems are designed by using binary systems

b) These systems are drawn and interpreted.

7. 	Problems will be able to be solved in ternary systems by using composition diagram.

a) Composition and temperature diagrams are defined in ternary systems.

- The formations of congruently-incongruently melted intermediate compounds and solid solutions are defined in ternary systems.

- Different reaction types are defined in ternary systems.

- Isothermal sections are drawn in ternary systems.

- Calculations on cooling and heating are done in ternary systems.

- Calculations of phase equilibrium diagram are done in ternary systems.

- Ternary systems are composed from binary systems.

- The terms of phase diagrams are applied in the ternary systems which are used in materials science and engineering field.

- These ternary systems are compared and interpreted to each other.

COURSE OUTLINE

Week 	1	Introduction:

The importance of phase diagram on materials science and engineering

Examine the relationship between thermodynamic and phase diagram

Week	 2-3	The main definitions and terms of phase diagrams:

- System, b) Phase, c) Equilibrium, d) Component, e) Degrees of freedom, f) Phase rule

Gibbs Phase Rule

Le Chatalier’s Principle

Unary systems (Single component systems):

- Pressure-temperature diagrams in unary systems

- Some, important unary systems used in materials science and engineering field

  - Water PT diagram

  - Carbon PT diagram

  - SiO2 PT diagram

Phase Transformations

- Simple Thremodynamics of Phase Transformations

- Types of Phase Transformations

Week	 4	Binary systems:

- Introduction to binary systems

- Simple binary systems without solid solubility

- Composition-temperature diagram in binary systems

- Lever Rule

- Isopleth studies of phase evolution

Week	5-6	Binary systems:

- Binary systems with intermediate compounds

- Studies of microstructural evolution using EPD

- Formation of congruently - incongruently melting compounds

- Phase calculations in binary systems which are used commonly

Week 	6-7	I. Midterm Exam

Week	7-8	Binary systems:

- Solid Solubility

- Investigating systems which have different compounds, solid solutions and reactions

- Composing binary systems by using (G-T diagrams

Week	8-9	Binary systems:

- Constructions of Phase Diagrams

- Composing binary systems by using (G-T diagrams

- Systems with unmixing

  - Zones of nucleation and growth

  - Spinodal decomposition

Week 	10	Polymer phase diagrams

- Liquid immiscibility

Weeek	10	II. Midterm Exam

Week 	10-11	Ternary systems:

- Composing ternary systems by using binary systems

- Introduction to ternary systems

- Determination of composition in ternary systems

- Explanation of Joins Alkamede Lines, Boundary Lines

- Determination of composition triangles and crystallization areas

Weeks	12	Ternary systems:

- Isothermal study in ternary systems

- Composing binary systems by using ternary systems

- Heating-cooling calculations on ternary systems

Weeks	13	Ternary systems:

a) Phase calculations in ternary systems which are used commonly

Week	14	Ternary systems:

a) Ternary solid solutions

Weeks	15	III. Midterm Exam

COURSE REQUIREMENTS

The students are required to attend to classes regularly, participate in discussions and also prepare themselves for the next lecture from their text book.

ASSESSMENT and EVALUATION

Midterm 1	20%

Midterm II	25%

Midterm III	30%

Quiz and HW	20%

SUGGESTED BOOK

Bergeron C.G. & Risbud S. H. (1984). Introduction to Phase Equilibria in Ceramics, The American Ceramic Society, Inc.

M<F Berard and DR Wilder (1990) Fundementals of Phase Equilibria in Ceramic Systems

RECOMMENDED PREREQUISITE COURSES

ENS 202 Thermodynamics

ENS 205 Introduction to Materials Science

COURSE INSTRUCTOR

Prof. Dr. M. Ali GULGUN

FENS 2055