SABANCI UNIVERSITY

GLASS SCIENCE AND TECHNOLOGY COURSE

MAT 422 - 522

A senior level course devoted to the understanding of commercial (SLS) silicate glass as a material and its technology of production. A modular course taught in theory and practice in collaboration with the glass industry experts in Turkey.

Recommended reading:

- The Handbook of Glass Manufacture,  F.Tooley, Tooley, New York : Books for Industry, [1974]

- Fundamentals of Inorganic Glasses, A. K. Varshneya, Academic Press Inc. 1994, CA, USA

- Glasses and Their Applications, H.Rawson, The Institute of Metals, 1991

- Glass Furnaces Design, Construction and Operation, Wolfgang Trier, Socitety of Glass Technology, Sheffield, UK, 2000 (translated by K.L. Loewenstein from Glassschmelzöfen: Konstruktion und Betreibsverhalten, W. Trier, Springer Verlag, 1984).

- Handbook of Glass ed. by J. David Musgraves, Juejun Hu, Laurent Calvez, Springer 2019

Chapter 1:  Glass and Glassy State					Week #10 (March 6, 2023)

- Introduction

- History

- Definition of glass

- Glass formation

- Theories related to glass formation

Duration:  1 week / 3 lectures;					Instructor: Melek Orhon

Chapter 2: Glass Compositions and Properties                  Week #11, 12, 13, 14 &15 (March 13, 20, 27, April 3,10,2023)

- Glass compositions (March 13) by Melek Orhon

- Viscosity

  - Importance of viscosity in glass production

  - Factors affecting viscosity

- Density

- Thermal expansion

- Effect of composition on thermal expansion

- Temporary and permanent stresses

- Annealing

- Mechanical properties (March 20) by Melek Orhon

- Basic principles: Stress- strain, elasticity, etc.

- Mechanical strength of glass

- Griffith model

- Subcritical crack growth, dynamic/static fatigue

- Measuring strength

- Hardness

- Tempering

- Optical properties (March 27) by Melek Orhon

  - Glass and electromagnetic radiation

  - Absorption-transmission-reflection-dispersion-scattering in glass

  - Color generation

  - Decolorizing

  - Defining color (color coordinates)

- Surface Tension (April 3) by Atilla Ünsal

- Thermal and Electrical Properties

  - Heat capacity

  - Thermal conductivity and Heat transfer

  - Electrical conductivity

- Combustion

- Glass Surface & Chemical Durability (April 10) by Melek Orhon

  - Definition of surface

  - Structure of glass surface and bulk glass

  - Formation of glass surface

- Corrosion reactions/weathering

- Effect of chemical composition and temperature

- Dishwasher resistance

Duration: 5 weeks/ 15 lectures;		                       Instructors: Melek Orhon, Atilla Ünsal

Mid-term Exam #1                                                                                              Week #16 (April 17, 2023)

Chapter 3: Raw Materials

Week #16  (April 17, 2023)

- Raw materials

- Common raw materials

- Raw material specifications

- Batch Calculations

Duration: 1 week / 2 lectures;			Instructor: Melek Orhon

Chapter 4:  Glass Melting 						Week # 17, 19 ( April 24 & May 8 2023)

- Glass Redox

- Definition

- Glass redox and color

- Calculating/ measuring redox

- Melting

  - Batch melting

  - Melting energy

  - Parameters affecting reaction rates (Melting temperature, particle size of raw materials, glass composition)

- Fining

  - Gases in glass (physical and chemical dissolution)

  - Formation of bubbles

  - Bubble removal (primary and secondary fining)

  - Bubbles as a defect in glass

- Homogenizing

- Conditioning

Duration: 2 weeks / 6 lectures; 					Instructor: Melek Orhon

Chapter 5: Furnace Technology				Week # 20, 21, 22  (May 15, 22 & 29 2023)

Batch preparation

  - Properties of granular materials

  - Bulk solids

  - Preparation of raw materials

  - Handling and transport

  - Segregation

  - Batch plants

  - Dosing

  - Mixing

  - Batch charging

- Furnace Types - Discontinuous/Continuous

- Furnace Structure – Refractories, steelwork

- Heat transfer/Heat exchangers (Regenerator/Recuperators)

- Combustion and firing

- Electric heating and furnaces

- Energy management

- Environmental issues and abatement

- Emerging melting technologies

- Glass Forming – Floating, fiberizing, moulding (PB/PP/NNPB)

- Course Review & QA

Duration: 3 weeks/ 9 lectures;				                               Instructor: Atilla Ünsal

Mid-term Exam #2                                                                                 Week # 23                                     Date TBA

Term Project                                                                                           Submission & Presentation       Date TBA

Quizzes %25, Midterms % 25 each, Term Project %25